## Slide 1
Establishing Independent Tunability of the Mechanical and Transport Properties of Polymer Gels
Lucas Rankin
MS Chemical Engineering ‘21

## Slide 2: Overview & Applications
Tunable solute transport
Mechanical Robustness
Coupled

## Slide 3: Our Approaches
Blend triblock/diblock copolymers at constant polymer concentration
Alter solvent viscosity

## Slide 4: Exchanging Triblock/Diblock Copolymers

## Slide 5: Effects on Gel Network Structure

## Slide 6: Effect of Wtri on Stress-Strain Behavior
wp = 20 wt%
Wtri as indicated
Data fit to 300% strain

## Slide 7: Effect of Wtri on Gel Stiffness

## Slide 8: Retained Mass Profiles

## Slide 9: Effect of Wtri on Transport Rate

## Slide 10: Altering Solvent Viscosity
Three gel series were fabricated
(6.6 wt%, 11.3 wt%, and 15.6 wt% SEBS polymer)

## Slide 11: Effect of Viscosity on Stress-Strain Behavior
Squalane=dotted lines
200 PO=dashed lines
380 PO=solid lines

## Slide 12: Effect of Viscosity on Gel Stiffness

## Slide 13: Effect of Viscosity on Retained Mass Profiles
11.3 wt%
380 PO
200 PO
Squalane

## Slide 14: Gel Diffusivities

## Slide 15: Conclusions
Blend triblock/diblock copolymers
  Tunes mechanics, not transport
Alter solvent viscosity
  Tunes transport, not mechanics
Using both approaches allows for independent property tuning!

## Slide 16: Acknowledgements
Dr. Kenny Mineart
Bucknell ChemE Dept.
Mineart Research Group

## Slide 17: Measuring Solute Transport
wp = 20 wt% and Wtri = 80 wt%

## Slide 18: Characterizing Gel Mechanics
Quasi-static (1%/sec) uniaxial tensile testing to 500% strain

## Slide 19: Characterizing Gel Mechanics
Uniaxial tensile testing
  To 500% strain
  Quasi-static (1%/sec)
  Slip-tube network model (STN)
Crosslinked
Network
=+
Entangled
Chains
STN

## Slide 20: SAXS Results
Only network connectivity changes

## Slide 21: Structural Characterization via SAXS
dPS-PS
rcr

## Slide 22: Additional SAXS Profiles
Wp= 10 wt%
Wp= 30 wt%

## Slide 23: Additional Stress-strain Profiles
Wp= 10 wt%, 1 wt% AOT
Wp= 30 wt%, 1 wt% AOT

## Slide 24: Gel Swelling
Wtri
X 100 wt%
▼ 90 wt%
▲ 80 wt%
♦ 70 wt%
■ 60 wt%
● 50 wt%

## Slide 25: Additional Release Profiles
6.6 wt%
15.6 wt%
Experimental (points):○ squalane, □ 200 PO, Δ 380 PO
Model Fits (lines): Dotted squalane, Dashed 200 PO, Solid 380 PO

## Slide 26: Diffusion Model Derivation
  Assume constant properties
  Simplify based on problem setting
2D Diffusion:

## Slide 27: Scaling of Diffusion Model
2D Diffusion:
  , , is half thickness
Scaled version:
1D Diffusion:

## Slide 28: Solving 1D Diffusion
  IC: 
  BC#1: 
  BC#2:  
    *Assume Bi>>>1

## Slide 29: Forms of the Solution
  Approximate using n=1 term (b/c exponential decay, n=1 dominates)

## Slide 30: SAXS Model
Δρi­ accounts for scattering density contrast
(q-dependent form factor)
Scr(q) is crosslink domain structure factor